OIL CONDITION MONITORING REPORT SLNS VIJAYABAHU

| GENERATOR PARTCULARS (Information provided by the customer) |  |  |
| --- | --- | --- |
|  | SSDG (Port) |  |
| Make : | Electro-Motive Division |  |
| Model : | 8-645E6 |  |
| Sr.No’s: | 70-H1-1044 |  |
| Date sampling : | 01 Aug 25 | 04 Aug 25 |
| Sampling point : | Lub oil sump |  |
| Sampling Method : | Extraction |  |
| Type of Lubricant : | Shell Gadinia S3 SAE 40 |  |
| System Capacity : | 250 US gal |  |

| RUNNING HRS DETAILS (Information provided by the customer) |  |  |
| --- | --- | --- |
|  | SSDG (Port) |  |
| Sample ID | M010555 | M010556 |
| Oil Running Hours | - | 04.00 |
| Total Running Hours of the Machinery | 137,939.00 | 137,943.00 |

ANALYSIS RESULTS

| Description | Method | Uncertainty (K=2) | Fresh Oil (As per the provided fresh oil sample) | SSDG (Port) |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | S/I-M010555 | S/I-M010556 |
| Viscosity @ 40oC(cSt) | ASTM D 445 | 0.006 | 128.00 | 128.13 | 128.07 |
| Viscosity @ 100oC (cSt) |  | 0.005 | 13.70 | 13.77 | 13.80 |
| Viscosity Index | ASTM D 2270 | N/A | 103 | 103.84 | 104.33 |
| Total Base No. mg KOH/g | ASTM D 4739 | 0.77 | 10.48* | 9.85 | 9.80 |
| Flash Point (cº) | ASTM D 92 | 0.026 | 230 | 228 | 228 |
| Water content % | ASTM D 95 | 0.082 | < 0.2 | <0.1 | <0.1 |

* Results were extracted from a fresh oil sample tested at MTTU laboratory as per ASTM D 4739 method.

Elemental Concentration as per ASTM D5185 (ppm)

| Element | Maximum Permissible Limit | Fresh Oil Sample | Uncertainty (K=2) | SSDG (Port) |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | S/I-M010555 | S/I-M010556 |
| Fe | 80 | < 1.000 | 0.15 | N/C | 3.804 |
| Cr | 10 | < 1.000 | 0.18 | N/C | < 1.000 |
| Si | 15 | < 1.000 | 0.17 | N/C | < 1.000 |
| Al | 20 | < 1.000 | 0.28 | N/C | 1.050 |
| Pb | 20 | < 1.000 | 0.13 | N/C | 1.413 |
| Cu | 25 | < 1.000 | 0.17 | N/C | 1.358 |
| Sn | 10 | < 1.000 | 0.20 | N/C | < 1.000 |
| Ni | 10 | < 1.000 | 0.08 | N/C | < 1.000 |

TREND ANALYSIS WITH PREVIOUS REPORT

|  |  |  | Fresh Oil Sample |  |  | SSDG (Port) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | S/I-M005482 | S/I- M00571 | S/I- M00574 | S/I- M00590 | S/I- M00596 | S/I- M00599 | S/I- M00606 | S/I-M00611 | S/I-M006173 | S/I- M006248 | S/I-M006378 | S/I-M006512 | S/I- M006529 | S/I- M006598 |
| Oil Running Hrs |  |  | - |  |  | 1001.26 | 1546.0 | 1787.5 | 2139.52 | 2456. | 2706. | 2956 | 3089.39 | 3206.29 | 3437.72 | 3687.32 | 3937.00 | 4187.00 | 4270.31 |  |
| T/R/H of Machinery |  |  | - |  |  | 129046 | 129591 | 129833 | 130185 | 130501 | 130751 | 131001 | 131135 | 131251.54 | 131483.12 | 131733.12 | 131983.12 | 132233.12 | 132324.71 |  |
| Viscosity @ 40oC (cSt) |  |  | 131.49* |  |  | 122.44 | 132.49 | 131.43 | 129.82 | 131.73 | 132.03 | 132.04 | 131.05 | 132.11 | 131.02 | 134.38 | 133.42 | 126.95 | 124.04 |  |
| Viscosity @ 100oC (cSt) |  |  | 14.52* |  |  | 13.37 | 13.95 | 13.80 | 13.74 | 13.96 | 14.01 | 14.02 | 14.09 | 14.01 | 13.68 | 13.78 | 14.11 | 13.50 | 13.34 |  |
| Viscosity Index |  |  | 110.25 |  |  | 104.19 | 102.01 | 101.09 | 101.80 | 102.88 | 103.21 | 103.33 | 105.18 | 103.14 | 104.91. | 98.31 | 103.20 | 104.25 | 102.13 |  |
| Total Base No (mgKOH/g) |  |  | 9.02* |  |  | 9.36 | N/C | 9.98 | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C |  |
| Flash Point (oC) |  |  | 220* |  |  | 190 | N/C | 190 | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C |  |
| Water content (%) |  |  | <0.2 |  |  | <0.1 | N/C | <0.1 | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C | N/C |  |
|  |  | Elemental Concentration as per ASTM D5185 (ppm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Element | Max. Permissible |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fe | 80 |  |  | < 1.000 |  | 10.283 | 7.076 | 6.562 | 5.177 | 5.005 | 1.415 | 9.994 | 7.059 | 8.150 | 2.526 | 5.534 | 15.937 | 6.584 | 4.867 |  |
| Cr | 10 |  |  | < 1.000 |  | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 |  |
| Si | 15 |  |  | < 1.000 |  | 7.549 | 5.833 | 10.671 | 6.998 | 3.733 | < 1.000 | 12.203 | 5.240 | 5.915 | 2.045 | 4.877 | 14.034 | 4.291 | 3.810 |
| Al | 20 |  |  | < 1.000 |  | 1.806 | 3.386 | 3.513 | < 1.000 | < 1.000 | < 1.000 | 9.787 | 2.912 | 9.103 | 2.500 | 2.233 | 11.284 | 1.699 | 2.043 |
| Pb | 20 |  |  | < 1.000 |  | 6.754 | 13.156 | 6.453 | 19.800 | 11.966 | 10.332 | 15.275 | 10.734 | 4.175 | 5.413 | 3.481 | 4.178 | 4.185 | 3.25 |  |
| Cu | 25 |  |  | < 1.000 |  | 10.371 | 12.737 | 1.067 | 14.809 | 15.757 | 13.437 | 15.546 | 9.717 | 16.762 | 12.789 | 13.296 | 15.678 | 15.720 | 14.096 |  |
| Sn | 10 |  |  | < 1.000 |  | 2.606 | 2.928 | <1.000 | 2.721 | 2.856 | 3.242 | 3.628 | 3.009 | 3.794 | < 1.000 | 2.023 | < 1.000 | < 1.000 | 3.2 |
| Ni | 10 |  |  | < 1.000 |  | < 1.000 | N/C | N/C | N/C | N/C | N/C | < 1.000 | < 1.000 | < 1.000 | N/C | N/C | < 1.000 | < 1.000 | < 1.000 |
| Fresh Oil Sample; SSDG (Port). S/I- M006709; M006781; S/I- M006882; S/I- M006991; S/I- M007107; S/I- M007233; S/I- M007439; S/I- M007517; S/I- M007834; S/I- M008075; Fresh Oil Sample; S/I- M008213; S/I- M008259; S/I- M008492; S/I- M008505; S/I- M008605; S/I- M008764; S/I- M008806; S/I- M008967; S/I- M009196; S/I- M009217. Oil Running Hrs; -; 4520.31; 4770.20; 5012.20; 5226.55; 5,491.35; 5741.35; 5991.35; 6241.35; 6491.35; 6741.35; -; 6991.35; 7,258.45; 7508.45; 7758.45; 7991.35; 8241.35; 8429.40; 8679.40; 8679.40; 9179.40. T/R/H of Machinery; -; 132574.71; 132,824.40; 133066.40; 133281.15; 133,531.15; 13378.15; 134031.15; 134281.15; 134531.15; 134781.15; -; 135,031.15; 135,281.15; 135,531.15; 135,781.15; 136031.15; 136281.15; 136469.20; 136,719.20; 136969.20; 137,219.20. Viscosity @ 40oC (cSt); 131.49*; 131.48; 129.27; 132.66; 129.50; 130.72; 134.42; 132.49; 129.14; 127.36; 130.26; 128.00; 135.36; 123.22; 132.98; 133.07; 131.94; 130.59; 133.83; 131.24; 132.43; 131.80. Viscosity @ 100oC (cSt); 14.52*; 14.00; 13.38; 13.04; 13.66; 13.88; 14.37; 14.09; 13.54; 13.73; 13.56; 13.70; 14.39; 13.27; 13.87; 13.26; 13.20; 13.40; 14.39; 13.95; 14.08; 13.70. Viscosity Index; 110.25*; 103.63; 97.82; 90.43; 101.08; 102.80; 105.52; 103.81; 99.85; 104.10; 99.151; 103; 104.89; 101.98; 100.55; 93.013; 93.20; 96.93; 106.32; 103.19; 103.753; 99.48. Total Base No. mgKOH/g; 9.02*; N/C; N/C; N/C; 9.30; 9.03; 8.94; 8.79; 8.42; 8.10; 7.90; 10.48*; 6.73; 6.88; 6.76; 6.68; 6.84; 6.95; 7.10; 7.28; 7.26; 7.19. Flash Point (oC); 220*; N/C; N/C; N/C; 200; 190; 190; 190; 190; 190; 192; 230; 218; 214; 218; 216; 214; 214; 216; 218; 218; 216. Water content%; < 0.2*; N/C; N/C; N/C; < 0.1; < 0.1; <0.1; <0.1; <0.1; <0.1; < 0.1; < 0.2; < 0.1; < 0.1; < 0.1; < 0.1; < 0.1; < 0.1; < 0.1; <0.1; <0.1; <0.1. Elemental Concentration as per ASTM D5185 (ppm). Element; Max. Permissible Limit. Fe; 80; < 1.000; 6.076; 11.925; 10.030; 8.263; 8.149; 7.555; 7.425; 9.038; 10.18; 5.470; < 1.000; 11.122; 12.137; 9.610; 7.703; 8.591; 13.258; 7.130; 7.058; 6.906; 7.671. Cr; 10; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; 1.149; 1.399; < 1.000; 1.425; 1.159; < 1.000; 1.577; 1.387; < 1.000; < 1.000; < 1.000; 1.979; < 1.000; < 1.000; 1.207; < 1.000. Si; 15; < 1.000; 5.664; 14.652; 10.531; 8.201; 5.027; 3.556; 3.874; 6.188; 7.683; 1.453; < 1.000; 5.595; 6.871; 3.725; 3.449; 4.549; 4.136; 1.121; 6.465; < 1.000; < 1.000. Al; 20; < 1.000; 2.723; 6.398; 3.350; 3.607; < 1.000; < 1.000; < 1.000; 1.322; 1.476; <1.000; < 1.000; 1.589; 1.540; < 1.000; < 1.000; < 1.000; 2.442; 1.000; 1.277; < 1.000; < 1.000. Pb; 20; < 1.000; 5.259; 4.710; 6.539; 4.818; 4.619; 4.173; 3.938; 4.528; 4.586; 3.563; < 1.000; 4.708; 5.370; 4.902; 3.839; 4.089; 2.424; 3.723; 3.831; 3.922; 4.160. Cu; 25; < 1.000; 14.656; 19.659; 17.955; 18.122; 13.425; 20.103; 15.290; 17.731; 17.222; 10.817; < 1.000; 18.984; 22.194; 22.025; 17.653; 19.136; 9.070; 15.309; 16.225; 16.492; 15.399. Sn; 10; < 1.000; 3.539; 4.401; 4.822; 4.603; 3.542; 3.102; 2.689; 3.676; 3.441; 2.451; < 1.000; 4.509; 5.162; 5.465; 4.358; 4.568; 2.476; 3.636; 4.219; 4.299; 4.570. Ni; 10; < 1.000; N/A; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; <1.000; <1.000; N/C; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000; < 1.000. |

|  |  | SSDG (Port) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Fresh Oil Sample | S/I- M009300 | S/I- M009521 | S/I- M009849 | S/I- M010555 | S/I- M010556 |
| Oil Running Hrs |  |  | 9,429.40 | 9,679.40 | 9,771.45 | - | 04.00 |
| T/R/H of Machinery |  |  | 137,469.20 | 137,719.20 | 137,811.25 | 137,939.00 | 137,943.00 |
| Viscosity @ 40oC (cSt) |  | 128.00 | 130.50 | 131.59 | 130.49 | 128.13 | 128.07 |
| Viscosity @ 100oC (cSt) |  | 13.7 | 13.77 | 14.27 | 14.01 | 13.77 | 13.80 |
| Viscosity Index |  | 103 | 101.58 | 106.96 | 104.69 | 130.87 | 104.33 |
| Total Base No. mgKOH/g |  | 10.48* | 7.32 | 7.30 | 7.10 | 9.85 | 9.80 |
| Water content% |  | < 0.2 | < 0.1 | <0.1 | <0.1 | 228 | 228 |
| Flash Point (oC) |  | 230 | 214 | 214 | 212 | <0.1 | <0.1 |
| Elemental Concentration as per ASTM D5185 (ppm) |  |  |  |  |  |  |  |
| Element | Max. Permissible Limit |  |  |  |  |  |  |
| Fe | 80 | < 1.000 | 6.346 | 7.770 | 6.167 | N/C | 3.804 |
| Cr | 10 | < 1.000 | 1.234 | 1.361 | < 1.000 | N/C | < 1.000 |
| Si | 15 | < 1.000 | < 1.000 | < 1.000 | 2.322 | N/C | < 1.000 |
| Al | 20 | < 1.000 | 1.058 | 3.542 | < 1.000 | N/C | 1.050 |
| Pb | 20 | < 1.000 | 4.226 | 4.190 | 4.889 | N/C | 1.413 |
| Cu | 25 | < 1.000 | 15.639 | 20.382 | 16.595 | N/C | 1.358 |
| Sn | 10 | < 1.000 | 3.918 | 4.160 | 4.259 | N/C | < 1.000 |
| Ni | 10 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | N/C | < 1.000 |

Wear Metals

# SSDG (Port)

ppm

| Element | Maximum Permissible Limit |
| --- | --- |
| Fe | 80 |
| Cr | 10 |
| Si | 15 |
| Al | 20 |
| Pb | 20 |
| Cu | 25 |
| Sn | 10 |
| Ni | 10 |

Total Running Hrs

Viscosity

# SSDG (Port)

At 400C

cSt

Total Running hrs

| Maximum permissible limit of Shell Gadinia S3 SAE 40 at 40oC | 160 cSt |
| --- | --- |
| Shell Gadinia S3 SAE 40 fresh oil viscosity value at 40oC | 128 cSt |
| Minimum permissible limit of Shell Gadinia S3 SAE 40 at 40oC | 96 cSt |

At 1000C

cSt

Total Running hrs

| Maximum permissible limit of Shell Gadinia S3 SAE 40 at 100oC | 17.125 cSt |
| --- | --- |
| Shell Gadinia S3 SAE 40 fresh oil viscosity value at 100oC | 13.70 cSt |
| Minimum permissible limit of Shell Gadinia S3 SAE 40 at 100oC | 10.275 cSt |