OIL CONDITION MONITORING REPORT SLNS SAYURA

| GEAR BOX PARTICULARS (Information provided by the customer) |  |
| --- | --- |
|  | Stbd Gear Box (No.01) |
| Make : | Renktack |
| Model : | ASL 69 GMBH |
| Sr.No’s: | 641182 |
| Sampling Date | 24 Feb 24 |
| Sampling point : | Lube oil sump |
| Sampling Method : | Extraction |
| Type of Lubricant : | Shell Gadinia S3 40 |
| System Capacity : | 450 Ltrs |

| RUNNING HRS DETAILS (Information provided by the customer) |  |
| --- | --- |
|  | Stbd Gear Box (No.01) |
| Sample ID | M007877 |
| Oil Running Hours | 2000.00 |
| Total Running Hours of the Machinery | 46652.55 |

ANALYSIS RESULTS

Viscosity

| Description | ASTM Method | Fresh Oil (As per OEM data sheet) | Uncertainty | Stbd Gear Box (S/I-M007877) |
| --- | --- | --- | --- | --- |
| Viscosity @ 40oC (cSt) | ASTM D 445 | 128.00 | 0.018 Cst | 129.48 |
| Viscosity @ 100oC (cSt) |  | 13.70 | 0.018 Cst | 13.92 |
| Viscosity Index | ASTM D2270 | 103 | N/A | 104.49 |

Elemental Concentration as per ASTMD 5185 (ppm)

| Element | Maximum Permissible Limit | Fresh Oil Sample | Uncertainty | Stbd Gear Box (S/I-M007877) |
| --- | --- | --- | --- | --- |
| Fe | 300 | < 1.000 | 2.191 | 14.842 |
| Cr | 15 | < 1.000 | 1.810 | < 1.000 |
| Si | 50 | < 1.000 | 1.021 | 9.323 |
| Al | 30 | < 1.000 | 1.107 | < 1.000 |
| Pb | 1500 | < 1.000 | 2.918 | 23.605 |
| Cu | 250 | < 1.000 | 1.064 | 17.734 |
| Sn | 50 | < 1.000 | 0.131 | < 1.000 |
| Ni | 30 | < 1.000 | 0.090 | < 1.000 |

N/A – Not Available

TREND ANALYSIS WITH PREVIOUS REPORTS

|  |  | Fresh Oil Sample | Stbd Gear Box |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | S/I- M000085 | S/I- M000776 | S/I- M002382 | S/I- M002852 | S/I- M005947 | S/I- M006010 | S/I- M006715 | S/I- M007877 |
| Oil Running Hrs |  | - | 1214.25 | 1849.50 | 3436.45 | 3935.05 | 673.25 | 760.15 | 1214.20 | 2000.00 |
| T/R/H of Machinery |  | - | 40867.20 | 41499.25 | 43089.40 | 43587.20 | 45326.20 | 45413.10 | 45867.15 | 46652.55 |
| Viscosity @ 40oC (cSt) |  | 128.00 | N/C | 139.17 | 101.89 | 128.24 | 124.25 | 127.63 | 127.57 | 129.48 |
| Viscosity @ 100oC (cSt) |  | 13.70 | N/C | 14.44 | 12.04 | 13.57 | 13.13 | 13.97 | 13.35 | 13.92 |
| Viscosity Index |  | 103 | N/C | 102.06 | 108.45 | 101.07 | 99.13 | 106.98 | 104.16 | 104.49 |
| Element | Max. Permissible Limit |  |  |  |  |  |  |  |  |  |
| Fe | 300 | < 1.000 | 2.388 | 11.883 | 5.898 | 3.985 | 3.469 | 3.952 | 3.611 | 14.842 |
| Cr | 15 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 |
| Si | 50 | < 1.000 | 3.608 | 7.611 | 4.162 | 2.302 | 3.534 | 3.589 | 2.965 | 9.323 |
| Al | 30 | < 1.000 | 3.272 | 3.151 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 |
| Pb | 1500 | < 1.000 | 5.969 | 3.478 | 5.017 | 10.223 | 24.223 | 15.356 | 8.880 | 23.605 |
| Cu | 250 | < 1.000 | 1.395 | 1.578 | < 1.000 | < 1.000 | < 1.000 | 1.004 | 1.229 | 17.734 |
| Sn | 50 | < 1.000 | 1.754 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 |
| Ni | 30 | < 1.000 | - | < 1.000 | < 1.000 | < 1.000 | N/C | N/C | N/C | < 1.000 |

N/A – Not Available

Wear Metals

Stbd Gear Box

ppm

Total Running Hrs