OIL CONDITION MONITORING REPORT SLNS SHAKTHI

| GEAR BOX PARTICULARS (Information provided by the customer) |  |
| --- | --- |
|  | Stbd Gear Box |
| Make : | SHICHUAN |
| Model : | GWC 3235 |
| Sr.No’s: | N/A |
| Date sampling : 13.02.2019 | 12 May 25 |
| Sampling point : | Lube Oil Sump |
| Sampling Method : | Extraction |
| Type of Lubricant : | Caltex Lanka Super 15 W 40 |
| System Capacity : | 45 Ltrs |

| RUNNING HRS DETAILS(Information provided by the customer) |  |
| --- | --- |
|  | Stbd Gear Box |
| Sample ID | M010154 |
| Oil Running Hours | 959.35 |
| Total Running Hours of the Machinery | 37647.55 |

ANALYSIS RESULTS

| Description | METHOD | Fresh Oil (As per OEM data sheet) | Uncertainty (K=2) | Stbd Gear Box |
| --- | --- | --- | --- | --- |
|  |  |  |  | S/I- M010154 |
| Viscosity @ 40oC (cSt) | ASTM D 445 | 109.4 | 0.006 | 84.62 |
| Viscosity @ 100oC (cSt) |  | 14.4 | 0.005 | 11.65 |
| Viscosity Index | ASTM D 2270 | 134 | N/A | 128.99 |
| Water contain % | ASTM D 95 | <0.2 | 0.082 | <0.1 |

Elemental Concentration as per ASTM D5185 (ppm)

| Element | Maximum Permissible Limit | Fresh Oil Sample | Uncertainty (K=2) | Stbd Gear Box |
| --- | --- | --- | --- | --- |
|  |  |  |  | S/I- M010154 |
| Fe | 300 | < 1.000 | 0.15 | 14.591 |
| Cr | 15 | < 1.000 | 0.18 | < 1.000 |
| Si | 50 | < 1.000 | 0.17 | < 1.000 |
| Al | 30 | < 1.000 | 0.28 | 1.185 |
| Pb | 1500 | < 1.000 | 0.13 | 4.788 |
| Cu | 250 | < 1.000 | 0.17 | 4.214 |
| Sn | 50 | < 1.000 | 0.20 | < 1.000 |
| Ni | 30 | < 1.000 | 0.08 | < 1.000 |

TREND ANALYSIS WITH PREVIOUS REPORTS

|  |  | Fresh oil sample | Stbd Gear Box |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | S/I-M000389 | S/I-M000926 | S/I-M002463 | S/I-M004167 | S/I-M006104 | S/I-M007847 | S/I-M008005 | Fresh oil sample | S/I-M010154 |
| Oil Running Hrs |  | - | 995.40 | 832.50 | 1030.05 | 867.35 | 283.20 | 500.00 | 531.45 | - | 959.35 |
| T/R/H of Machinery |  | - | 31595.25 | 32428.15 | 33269.55 | 35740.05 | 36156.10 | 36656.10 | 36688.20 | - | 37647.55 |
| Basic Properties |  |  |  |  |  |  |  |  |  |  |  |
| Viscosity @ 40oC (cSt) |  | 132.31 | N/C | 134.81 | 138.18 | 133.59 | 139.35 | 129.71 | 132.88 | 109.4 | 84.62 |
| Viscosity @ 100oC (cSt) |  | 14.4 | N/C | 14.16 | 14.30 | 14.23 | 14.81 | 14.07 | 13.60 | 14.4 | 11.65 |
| Viscosity Index |  | 97 | N/C | 102.54 | 101.24 | 104.56 | 106.46 | 106.24 | 97.45 | 134 | 128.99 |
| Water contain % |  | <0.2 | N/C | N/C | N/C | N/C | N/C | N/C | N/C | <0.2 | <0.1 |
| Elemental Concentration as per ASTM D5185 (ppm) |  |  |  |  |  |  |  |  |  |  |  |
| Element | Maximum Permissible Limit |  |  |  |  |  |  |  |  |  |  |
| Fe | 300 |  | 31.764 | 161.723 | 71.401 | 128.269 | 116.947 | 19.390 | 24.846 | < 1.000 | 14.591 |
| Cr | 15 |  | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 |
| Si | 50 |  | 3.844 | 6.724 | 7.926 | 3.414 | 9.536 | < 1.000 | < 1.000 | < 1.000 | < 1.000 |
| Al | 30 |  | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | 1.185 |
| Pb | 1500 |  | 5.801 | 13.258 | 7.984 | 3.432 | 20.619 | 5.855 | 10.033 | < 1.000 | 4.788 |
| Cu | 250 |  | 4.954 | 14.061 | 12.373 | 3.948 | 34.856 | 6.879 | 12.181 | < 1.000 | 4.214 |
| Sn | 50 |  | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 | < 1.000 |
| Ni | 30 |  | < 1.000 | < 1.000 | < 1.000 | < 1.000 | N/A | < 1.000 | < 1.000 | < 1.000 | < 1.000 |

Wear Metals

(ppm)

Total Running Hrs

Total Running Hrs

Viscosity

400C								1000C

(cSt)

(cSt)

Total Running Hrs

Total Running Hrs

Total Running Hrs